# LOXO AAC PANEL VENEER CLADDING SYSTEM

## 1.	GENERAL

This section relates to LOXO NZ LTD 50mm Panel Veneer Aerated Concrete wall cladding system with a plaster finish based on 50mm aerated concrete panels fixed to timber/metal framing on a drained / ventilated cavity.

### 1.1	RELATED WORK

Refer to ~ for ~.

### 1.2	ABBREVIATIONS AND DEFINITIONS

Refer to the general section 1232 INTERPRETATION & DEFINITIONS for abbreviations and definitions used throughout the specification.

The following abbreviations apply specifically to this section:

LNZ	Loxo Cladding NZ

MPNZA	Master Painters New Zealand Association

AAC	Autoclaved Aerated Concrete

LRV	Light reflective value

EPS	Expanded Polystyrene

LBP	Licensed Building Practitioner

Documents

### 1.3	DOCUMENTS

Refer to the Masterspec general section 1233 REFERENCED DOCUMENTS.  The following documents are specifically referred to in this section:

NZBC E2/AS1	External moisture

AS/NZS 1170.2	Structural design actions - Wind actions

AS 3566	Self-drilling screws for the building and construction industries

NZS 3602	Timber and wood-based products for use in building

NZS 3604	Timber-framed buildings

### 1.4	MANUFACTURER/SUPPLIER DOCUMENTS

Manufacturer's and supplier's documents related to this section are:

Loxo Cladding Systems Panel And Flooring Systems Technical Manual.

CodeMark Certificate of Conformity for Loxo Cladding Systems NZ Limited

System Certificate Number CM70065.

Materials and execution to Loxo NZ Ltd specification except where varied by this specification and supported by architectural detailing.

Masons and Wattyl Granosite external coatings supporting specifications

Copies of the above literature are available from:

Web:	www.loxocladding.co.nz

E-mail	info@loxocladdingco.nz

Telephone:	03 372 3343

Warranties

### 1.5	WARRANTY

LNZ warrant this system under normal environmental and use conditions against failure of materials and execution.  The plaster system is warranted as follows:

Materials:	15 years from date of practical completion issued by the manufacturer.

Execution:	5 years from the date of practical completion issued by the licensed Loxo contractor upon completion.

A warranty pack including a producer statement from the licensed Loxo contractor must be made available by the licensed contractor at the date of practical completion.

Requirements

### 1.6	NO SUBSTITUTIONS

Substitutions are not permitted to any specified LNZ plaster system.

### 1.7	QUALIFICATIONS

Use only applicators with NZ LBP External Plastering licenses to apply the exterior wall cladding system.

Documentation

### 1.8	FINISH SAMPLE

If requested submit one 300mm x 300mm sample of the selected finish texture and colour for review.  Obtain owners signature of acceptance on sample and return to the LBP licensed Loxo applicator.

### 1.9	MAINTENANCE INSTRUCTIONS

Provide LNZ maintenance instructions before practical completion of the contract for issuing to the building owner.

### ROUTINE CLEANING

Carry out routine trade cleaning of this part of the work as per LNZ Maintenance Guide, including periodic removal of all debris, unused and temporary materials and elements from the site.

### 1.10	HEALTH AND SAFETY

Refer to the requirements of the Health and Safety in Employment Act and OSH:

Guidelines for the provision of facilities and general safety in the construction industry.  If the elimination or isolation of potential hazards is not possible then minimise hazards in this work on site by using the proper equipment and techniques as required in the MPNZA Painters hazard handbook.  Supply protective clothing and equipment.  Inform employees and others on site of the hazards and put into place procedures for dealing with emergencies.  Obtain from LNZ the material safety data sheets for each product.  Keep sheets on site and comply with the required safety procedures.

Performance

### 1.11	PERFORMANCE

The LBP licensed Loxo applicator must accept responsibility for the structural and weather-tight performance of the exterior render application.

### 1.12	PROTECTION OF NEW PLASTER

Confirmation of the protection systems to be applied to fresh plaster coats to be agreed between the main contractor and the licensed applicator before plastering begins.

### 1.13	INSPECTIONS

Allow to inspect the whole of the work at each stage.  Determine a programme for inspections including notification when each part and stage of the work is ready for inspection prior to the work commencing.  Permit representatives from LNZ to inspect the work in progress and to take samples of their products from site.

### 1.14	PRODUCER STATEMENT

Provide a producer statement compiled by the LBP licensed Loxo applicator in the form as required by the Building Consent Authority.

### 1.15	FIXINGS, WIND

Design and use the fixings appropriate for the wind zone (R) and topographical classification (T) of this site and building height; as required by NZS 3604 and the wind loads on various wall areas as given by AS/NZS 1170.2.

## 2.	PRODUCTS

Materials

### 2.1	LOXO AAC PANELS

50mm or 75mm thick Autoclaved Aerated Concrete Panels measuring 600 mm x 2200 mm.

Plaster

### 2.2	CEMENTITIOUS RENDERS

Wattyl Granosite or Masons high quality factory-mixed polymer modified cement based plaster to NZS 4251.1.  Refer to SELECTIONS for type of render.

### 2.3	ACRYLIC TEXTURES

Durable high build water based Wattyl Granosite or Masons acrylic texture coating system.  Available in a wide range of finishes, builds and profiles.  Refer to Wattyl or Masons for full range of textures.

Components

### 2.4	LOXO PANEL FIXINGS, TIMBER FRAME

To AS 3566.  100mm long Corrosion Class 4 wood screws with a head diameter of 14mm and a shank diameter of 5.1mm.   To NZS 3604 defined Corrosion Zones B and C and Grade 304 stainless steel 6-gauge in Zone D and Zone E (NZBC E2/AS1).

### 2.5	LOXO PANEL ADHESIVE

Loxo Adhesive for bonding panel joints during construction prior to plastering.

### 2.6a	EXTERIOR CAVITY POLY BATTENS

40mm x 22-50mm x 1200mm EPS high density polystyrene battens.

### 2.6b	TIMBER CAVITY BATTENS

Fix 45mm x 20mm H3.2 timber battens full length to studs to achieve either a 20mm minimum thickness drained cavity to NZBC E2/AS1, 9.0 Wall claddings.  The battens are fixed by 50mm Ringshank nails which will penetrate the wall framing studs through the wall underlay.  Seal the top of the cavity.  Install cavity closer/vermin proofing at base of wall, open horizontal (or raking) junctions, over openings (windows, meters etc).  Horizontal cavity battens must be no longer than 100mm and fixed at a 15° slope.  Fix additional battens to internal and external corners and around openings to LNZ standard details.

### 2.7	REINFORCING MESH

### Wattyl Granosite Grano Mesh,150 g/m² alkali-resistant fibreglass woven mesh

### 4 x 4mm White Mesh or equivalent

### 2.8	PAINT

Wattyl Granosite GranoImpact 100% acrylic high performance elastomeric coating compatible with cement based plaster and suitable for textured surfaces. Approved to APAS 0118/2 & APAS 0117/3. Also accept Resene and Dulux Acratex equivalents.

### 2.9	PRIMER

Wattyl Granosite GranoPrime single pack water based primer to cementitious substrates.

Accessories

### 2.10	FLASHINGS AND ACCESSORIES

Proprietary profiles made from rigid uPVC for head, sill, and jamb flashings, 22mm U-channel, metal and uPVC vent grilles.

### 2.11	EXTERIOR CAVITY BASE BEAD

Proprietary cavity base shoe made from rigid uPVC.  Base bead to have 3mm x 40mm slots to provide 1000mm² ventilation per linear metre.

### 2.12	SEALANTS

Paintable MS sealant in accordance with LNZ's guide and set against backer rods where necessary.

### 2.13	FLEXIBLE FLASHING TAPES

Tapes covered by a valid BRANZ or BEAL appraisal for use as a seal pipe penetrations, fixing cleats etc.

2.14	WATERPROOF MEMBRANE LIQUID

ASA Bostik Dampfix Gold liquid applied waterproofing membrane for use on extended sill projections, over the top of plastered parapets.

### 2.15	ADHESIVE

AAC compatible polymer modified cement based mortar construction adhesive for adhering between Loxo Panels and  uPVC components to the Loxo Panel as and where required.

## 3.	EXECUTION

Conditions

### 3.1	DELIVERY

Keep plaster products dry in transit.  Take delivery of plaster products dry and undamaged.  Reject all damaged materials.

### 3.2	STORAGE

Deliver all materials in original unopened packaging with labels intact.  Provide dry storage on site, stack carefully, protect from mechanical damage.  Keep bagged render off concrete surfaces on a timber pallet or timber dunnage.  Plaster stock older than six months must be discarded.  Battens, uPVC flashings and profiles must be protected from direct sunlight and physical damage.

### 3.3	PLASTERING CONDITIONS

Carry out plastering to LNZ's specifications under conditions which will not adversely affect the finished work.

### 3.4	PROTECT

Before application of plaster, apply masking film and tape to all joinery, pipes, roofs and all areas likely to be marked by the plaster.  Use drop cloths and ground covers to keep the working areas clean.  Clean droppings off finished work immediately.

### 3.5	SUBSTRATE

Do not commence work until the framing is of the standard required for the specified finish; plumb, level and in true alignment.  Moisture content of timber framing must not exceed the requirements specified by NZS 3602 to minimise shrinkage and movement after the panels are fixed.  Studs are not to exceed 600mm centres and nogs fitted flush at a maximum of 800mm centres.  Wall underlay to comply with NZBC E2/AS1 Table 23.

For steel framing C section studs and nogs, the minimum section size to be 75mm x 32mm with a web thickness of 0.55mm.

### 3.6	LOXO PANEL SUBSTRATE

Do not commence work until openings and apertures have been cut, pipes, fixtures, fixing pads and plugs have been fixed and flashings and other preparations are complete.  All defects in substrate must be rectified prior to application of plaster coatings.  Ensure that backgrounds and adjoining surfaces are, after the preparation called for in this section, of LNZ's required standard.

### 3.7	FLASHING AND DETAILING

Comply with NZBC E2/AS1, 4.0 Flashings and LNZ's penetration flashing guidelines.  Carry out to the required standard of execution to ensure water does not penetrate.

### 3.8	CONFIRM LAYOUT

Before commencing work confirm the layout of expansion joints and other visual detailing of the finished work.

Application

### 3.9	PENETRATIONS

Confirm that exterior wall openings have been prepared ready for the installation of all window and door frames and other penetrations through the cladding.  Required preparatory work includes the following:

-	wall underlay to openings finished and dressed off with flexible flashing tape ready for the installation of window and door frames and other penetrations.

-	installation of window and door joinery.

-	installation of flashings (those required to be installed prior to installation of penetrating elements).

-	where electrical cables pass through cladding, put into conduit to ensure that there is no direct contact with the polystyrene battens.

-	windows must be installed so a gap of 23mm to 24mm is provided from the back of the joinery to the front of the timber framing.

-	all penetrations such as water pipes, ducting, light fittings, must be installed with a minimum of 5° outward slope and be sealed to the wall underlay by the contractor who installed them.

### 3.10	FLASHING AND ACCESSORIES

Fit flashings to jambs, sills and heads on recessed joinery using the manufacturer's proprietary flashings.  Reinforce external corners and bottom edges of Loxo Panel with uPVC angles and channel extrusions glued to the Loxo Panel with Sika Nailbond PB adhesive.

### 3.11	CAVITY BASE BEAD

Where the Loxo Panel system is applied in a 'free-hanging' state the bottom edge of the Loxo Panels can be additionally supported by fixing a 50mm high backed uPVC base bead to the bottom wall plate.

### 3.12	POLYSTYRENE CAVITY BATTENS

Fix polystyrene battens to studs to achieve a 20mm minimum thickness drained cavity to NZBC E2/AS1, 9.0 Wall claddings.  The battens are fixed flat head galvanised nails (3 per 1200mm batten length) which will penetrate the wall framing studs over the wall underlay.  Alternativley fix the battens to the building wrap over the studs with a construction adhesive. (consult Loxo NZ for approved adhesives). Seal the top of the cavity.  Install cavity closer/vermin proofing at base of wall, open horizontal (or raking) junctions, over openings (windows etc).  Horizontal cavity battens must be no longer than 100mm and fixed at a 5° slope.  Fix additional battens to internal and external corners and around openings to LNZ's standard details.

### 3.13	FIXING LOXO PANELS OVER CAVITY BATTENS

Screw fix through the cavity battens into the wall framing to LNZ's details.  Loxo Panels may be joined off stud but all sheet edges must be glued with Loxo Adhesive as the sheets are being installed prior to mesh coat being applied.  All corners must be castellated and vertical sheet joins to be offset by a minimum of 100mm.  Horizontal panel edges do not require edge fixing, except at soffits and at window and door openings where additional framing will be required.

### 3.14	SILLS BALUSTRADES AND PARAPET TOPS

A minimum slope of 15° to all horizontal surfaces. Except where metal cappings are used on balustrades and parapet tops. This fall is to comply with NZBC E2/AS1.

### 3.15	MOVEMENT CONTROL JOINTS

Incorporate in accordance with the design information supplied by LNZ.  Control joints to be constructed in the Loxo Panel in accordance with the Technical Literature and must be provided horizontally at 6m centres and at inter-storey levels and vertically at 6m centres.  Additional control joints will be required where the system abutments different cladding types, where cladding covers structural materials, and over a movement joint in the underlying framing.  Confirm locations in writing to the owner before work commences.

Finishing

### 3.16	PLASTERING

The plaster and paint system applied to Loxo Panel MUST be the Masons or Granosite system applied to manufacturers instructions.

Completion

### 3.17	CLEANING

Remove debris, unused materials and elements from the site relating to the plaster system application.  Replace damaged, cracked or marked elements.  Leave the whole of this work to the required standard.

### 3.18	FINAL INSPECTION

A final inspection by the licensed Loxo Panel contractor of the entire finished cladding to take place immediately after completion of the insulating wall cladding work and any defects or subsequent damage made good immediately.

## 4.	SELECTIONS

Substitutions are not permitted to the following, unless stated otherwise.

### 4.1	LOXO PANEL

Size/thickness:	2200mm x 600mm x 50mm (or 75mm thick)

### 4.2	CAVITY BATTENS

Polystyrene:	Classic Battens: 22mm x 40mm x 1200mm

Deluxe Battens: 50mm x 40mm x 1200mm

### 4.3	PANEL ADHESIVE

Brand:	Loxo Adhesive or Bostik FixAll Tile Adhesive

### 4.4	uPVC ADHESIVE

Brand:	Sika Nailbond PB adhesive or equivalent

### 4.5	REINFORCING MESH

Type:	Wattyl Granosite Grano Mesh,150 g/m² alkali-resistant fibreglass woven mesh.

Grade/weight:	4 x 4mm White Mesh

### 4.6	HIGH BUILD ACRYLIC TEXTURE FINISH

1st coat:	Granosite Grano Adhesive Mortar Coarse (with reinforcing mesh)

2nd coat:	Granosite Grano Adhesive Mortar Coarse

3rd coat:	Granosite GranoPrime

4th coat:	Granosite GranoAntique or GranoMarble

5th & 6th coat:	Granosite GranoImpact

### 4.7	GRANOSITE CEMENT BASED TEXTURE - SPONGE 1mm FINISH

1st coat:	Granosite Grano Adhesive Mortar Coarse (with reinforcing mesh)

2nd coat:	Granosite Grano Adhesive Mortar Coarse

3rd coat:	Granosite GranoSponge 1mm

4th coat:	Granosite GranoPrime

5th & 6th coat:	Granosite GranoImpact

4.8 	MASONS CEMENT BASED TEXTURE – SPONGE FINISH

### SEALER

Masons Plastaseal Sealer to assist with controlling suction during plastering application.

### BASE COAT

Factory-mixed polymer modified cement based plaster.

### LIGHTWEIGHT BASE COAT

Pre-mixed cement based plaster containing lightweight aggregates, adhesion and workability aids, together with polypropylene fibre reinforcement.

### FIBREGLASS MESH

150g/m² fibreglass mesh embedded in Basecoat.

### SKIMMING RENDER (LEVELLING COAT)

Skimming render.

### PLASTABRICK TEXTURE COAT

1mm Finishing Plaster.  Factory-mixed polymer modified cement based finishing plaster.

### ADOBE FINISHING PLASTER - POLYMER MODIFIED

Polymer modified cement based finishing plaster.

### LIMESTOP SEALER

Limestop sealer coat.

### PAINT SYSTEM

2 coats 100% acrylic high performance elastomeric.

3rd Coat Texture options for pre-mix, pre-coloured 100% acrylic emulsions include:

951 Tuscany Fine -Duspec NZSA 3540

951 Trowel On 2mm - Duspec NZSA 3545

951 Trowel On 1mm - Duspec NZSA 3544

952 Spray On 2mm - Duspec NZSA 3547

952 Spray On 1mm - Duspec NZSA 3546